## Slide 1
Francesco Sciortino
Sapienza Universita’ di Roma
http://www.roma1.infn.it/~sciortif/
“Entropy in Self-Assembly”
SISSA Seminar, April 28 2021
Thanks to Cristian Micheletti and Matteo Becchi

## Slide 2: Outline
Aims:
Entropy and Order, W (Hard-sphere crystallization, Onsager theory)
Entropy in the ground state (Networks, Crystal selection,Vitrimers).
Entropy attracts (Depletion interactions, Safran, DNA functionalized colloids)

## Slide 3
J. Chem. Phys. 27, 1208 (1957)
s

## Slide 4: Which one is more disordered ?

## Slide 5: Hard Spheres (HS) Equilibrium properties
Hard spheres present a fluid–solid phase separation due to entropic effects
s

## Slide 6
How do we understand HS crystallization ?
At constant V, we need to maximize the entropy
“Configurational” entropy (topological entropy)
Translational Entropy (cage entropy, vibrational)

## Slide 7: A proxy to translational Entropy...
MSD=|ri(t)-ri(0)|^2

## Slide 8
b
f=0.54
f=0.495

## Slide 9
Orientational Entropy
ANNALS NEW YORK ACADEMY OF SCIENCES 1949

## Slide 10
Isotropic-Nematic Transition (Onsager Theory)
Isotropic
Nematic
n

## Slide 11
φI−N =4D/L
g=90
g=0
significant reduction of sampled
phase space !!!!
Free energy= Ideal gas + first virial correction

## Slide 14
Entropy and flexibility
(translation+rotation)
Entropy of the Ground State
if the liquid reaches a fully bonded state, then it has the same energy of the crystal !

## Slide 15
Examples of patchy particles

## Slide 16
fig1a_wertheim_T0.06.eps
A limited valence colloid: The DNA nanostar
www.pnas.org/cgi/doi/10.1073/pnas.1304632110

## Slide 17
All particles
are bonded with
four neighbours
There are loops
of different
length
Particles
“vibrate”
around equilibrium
positions.

## Slide 18
How about (low density) crystals ?
Entropy decides the most stable phase (exactly as in HS!)
Competition between:
Number of microstates accessed at fixed bonding” (vibrational entropy) (Svib)
- Number of different bonding topologies (configurational entropy) (Sconf)
Sxt –Sfluid

## Slide 19
Sxt --- Crystal Vibrational Entropy Svib
Sfluid --- Fluid Vibrational Entropy Svib+
Fluid Configurational Entropy Sconf
Sxt –Sfluid
Increasing the bond angle (flexibility) increases both entropies…..
Same rate ?
flexibility
flexibility

## Slide 21
On increasing flexibility: Ultrastable liquids !

## Slide 22
Large flexibility of the angular interactions: (wide variety of networks, increasing Sconf)
Low valence. Small density of the coexisting liquid phase
Key elements for liquid stability at T=0 K:
(ultrastable liquids !)
Thermodynamically stable !

## Slide 23: Crystal Selection by Entropy
J. Chem. Phys 132, 184501 2010
Diamond
BCC
(2 interpenetrated
diamond)
Pressure=0

## Slide 24: Crystal Selection by Entropy

## Slide 25: Crystal Selection by Entropy
”regular structure”
”less regular structure”

## Slide 26
Spheres
(S)
Octahedra
(M)
Mixed Spheres+
Octahedra (R)

## Slide 29: Entropic Attraction Large HS in a bath of small HS
Which distance is
most probable ?

## Slide 32: Rd
qo
qo
r/2
Same story from a different perspective

## Slide 33
Real hard-spheres

## Slide 34: Visualizzation of depletion forces
A.D. Dinsmore, P. B. Warren, W. C. K. Poon, and A. G. Yodh,
EPL 40, 337 (1997).
Phase separation of a bidisperse sphere mixture:
rb= 413nm, rs= 35nm,
Volume fraction: Φb= 0.02
(visible),
(not resolved)

## Slide 35
For depletion interactions, arrest at low f (gelation) is the result of a phase separation process interrupted by the glass transition
CONFOCAL
IMAGES
First Order Transition

## Slide 36: Depletion: shape and roughness

## Slide 37
Another example

## Slide 42
Playing with the properties of the co-solute
Depletant Shape...

## Slide 43
Polymerizing solvent ...

## Slide 45: Safran’s attraction
A network ?
.. a gas of isolated droplets ?
... or ....
Another important
source of entropy:
Combinatorial Entropy

## Slide 47
Oleg Gang (Brookhaven and Columbia)
------CGCG
------CGCG
Another important
source of entropy:
Combinatorial Entropy

## Slide 48
Can we quantify the entropic gain ?
A coarse-grained version of the
DNA-decorated gold nanoparticle

## Slide 49
W=(N− 1)!!
W=(N− 1)!!
W=(2N− 1)!!
N RED + N YELLOW
Reactive sites

## Slide 50
Umbrella sampling based
evaluation of the effective potential

## Slide 54
Catalyst … Arrhenius Dynamics
“Strong glass former”

## Slide 55
Wertheim theory: free energy
Using thermodynamic perturbation theory, we can approximate the (Helmholtz) free energy of the model system.
Free energy change as a result of forming bonds, in the limit of T going to zero (strong bonds):
Combinatorial entropy term:

## Slide 56
Entropy in Theory and Simulation: comparison
Comparison between the entropy from simulations (red) and theory (blue).
Number density
composition
Entropy per particle

## Slide 57
T=0 K Equilibrium phase diagram (Entropy Only!)
Theory: black dashed line
Simulations: points, solid line
Placing a vitrimer network in a good solvent leads to swelling
The network phase is closer to the ideal x
the network never fully dissolves

## Slide 59
R
Thanks for your attention !

## Slide 60
Attracting without phase separating (hyper-branched)

## Slide 61
One unreacted site (A) per cluster
Only sol-phase (the infinite cluster
appears only when pA=1)
No gas-liquid phase separation can
exist.
When pA=1, there is
one percolating cluster,
independently on density
(Flory-Stockmayer mean-field results)
Strong assumption:
no intra-cluster bonds

## Slide 62
Intra-cluster bonds !
OxDNA based MD simulations

## Slide 63
OxDNA
High T
Intermediate T
Low T

## Slide 67: a=10, f(q)
q
f(q)

## Slide 69
55
5
1
DashedIsotropic
Full Nematic

## Slide 72: Another interesting soft-matter case
DNA-grafted gold nanoparticles
(palindromic sticky sequences)

## Slide 76
Asakura, S., Oosawa,F, On Interaction between Two Bodies Immersed in a Solution of Macromolecules, JCP 22 (7): 1255 1954.
Small-small
Small-large

## Slide 80
2

## Slide 82
Sterically stabilized PMMA particles (polydispersity 5-10 %)
Courtesy P. Pusey

## Slide 83
The patchy model analog
Bonding volume and energy scale….

## Slide 84
Connections to patchy particle
Network formed by a mixture of particles with valence f1 and f2 in non-stochiometric ratio in
which all possible bonds between particles of different type are present!
Where is T ? T=0 K !
What does it mean to switch ? Explore the different
configurations of the ground state
There is life in the ground state !

## Slide 85
Self complementary DNA sequences