## Slide 1
Bangalore, June 2004
Potential Energy Landscape Description of Supercooled Liquids and Glasses

## Slide 2
Why do we case ? Thermodynamics and Dynamics
Review of thermodynamic formalism in the PEL approach
Comparison with numerical simulations
Development of an PEL EOS
Extention to non-equilibrium case (one or more fictive parameters ?)
Outline

## Slide 3: Why do we care: Dynamics
Why do we care ? Dynamics
P.G. Debenedetti, and F.H. Stillinger, Nature 410, 259 (2001).
A slowing down that cover more than 15 order of magnitudes

## Slide 4: Why do we care Thermodyanmics
Why do we care: Thermodynamics
A vanishing of the entropy difference at a finite T ?

## Slide 5: Separation of time scales
van Megen and S.M. Underwood
Phys. Rev. Lett. 70, 2766 (1993)
(t)
(t)
log(t)
Supercooled Liquid
Glass

## Slide 6: Citazioni goldstein, stillinger

## Slide 7: Potential Energy Landscape, a 3N dimensional surface
IS
P
e
IS

Statistical description of the number, depth and shape
of the PEL basins
The PEL does not depend on T The exploration of the PEL depends on T

## Slide 8: Z(T)=  Zi(T)
fbasin i(T)= -kBT ln[Zi(T)]
all basins i
fbasin i(T)= eIS+ kBTln [hj i/kBT]
+ fanharmonic i (T)
normal modes j

## Slide 9: Stillinger formalism

## Slide 10: Thermodynamics in the IS formalism
Stillinger-Weber
F(T)=-kBT ln[(<eIS>)]+fbasin(<eIS>,T)
with
fbasin(eIS,T)= eIS+fvib(eIS,T)
and
Sconf(T)=kBln[(<eIS>)]
Basin depth and shape
Number of explored basins

## Slide 11: 1-d Cos(x) Landscape

## Slide 12: Didattic - Correlation Function in IS

## Slide 13: Specific Heat

## Slide 14: Specific Heat
Time-Dependent Specific Heat in the IS formalism

## Slide 15: Real Space
rN
Distribution of local minima (eIS)
Vibrations (evib)
+
eIS
evib
Configuration Space

## Slide 16: From simulations…..
F(T)=-kBT ln[(<eIS>)]+fbasin(<eIS>,T)
<eIS>(T) (steepest descent minimization)
fbasin(eIS,T) (harmonic and anharmonic contributions)
F(T) (thermodynamic integration from ideal gas)
E. La Nave et al., Numerical Evaluation of the Statistical Properties of
a Potential Energy Landscape, J. Phys.: Condens. Matter 15, S1085 (2003).

## Slide 17: minimization

## Slide 18: Eis nel tempo
BKS Silica

## Slide 19: Evaluete the DOS
diagonalization

## Slide 20: Harmonic Basin free energy
Very often approximated with……

## Slide 21: Vibrational Free Energy
SPC/E
LW-OTP
 ln[i(eIS)]=a+b eIS
kBTjln [hj(eIS)/kBT]

## Slide 22: Pitfalls

## Slide 23: anharmonic
f anharmonic
eIS independent
anharmonicity
Weak eIS dependent
anharmonicity

## Slide 24: Einstein Crystal

## Slide 25
Caso r2 per
n-2n

## Slide 26: The Random Energy Model for eIS
Hypothesis:
Predictions:
eIS)deIS=eN -----------------deIS
e-(eIS -E0)2/22
22
 ln[i(eIS)]=a+b eIS
<eIS(T)>=E0-b2 - 2/kT
Sconf(T)=N- (<eIS (T)>-E0)2/22

## Slide 27: Gaussian Distribution ?
eIS=eiIS
E0=<eNIS>=Ne1IS
2= 2N=N 21

## Slide 28: T-dependence of <eIS>
SPC/E
LW-OTP
T-1 dependence observed in the studied T-range
Support for the Gaussian Approximation

## Slide 29: P(eIS,T)

## Slide 30: BMLJ Sconf
BMLJ Configurational Entropy

## Slide 31: T-dependence of Sconf (SPC/E)

## Slide 32: The V-dependence of , 2, E0
eIS)deIS=eN -----------------deIS
e-(eIS -E0)2/22
22

## Slide 33: Landscape Equation of State
P=-∂F/∂V|T
F(V,T)=-TSconf(T,V)+<eIS(T,V)>+fvib(T,V)
In Gaussian (and harmonic) approximation
P(T,V)=Pconst(V)+PT(V) T + P1/T(V)/T
Pconst(V)= - d/dV [E0-b2]
PT(V) =R d/dV [-a-bE0+b22/2]
P1/T(V) = d/dV [2/2R]

## Slide 34: Developing an EOS based on PES properties

## Slide 35: SPC/E P(T,V)=Pconst(V)+PT(V) T + P1/T(V)/T
FS, E. La Nave, and P. Tartaglia, PRL. 91, 155701 (2003)

## Slide 36
Eis e S conf for silica…
Esempio di forte

## Slide 37: AG per Silica
Correlating Thermodynamics and Dynamics: Adam-Gibbs Relation
BKS
Silica
Ivan Saika-Voivod et al, Nature 412, 514 (2001).

## Slide 38: V ~ (/r)-n
Soft Spheres with different softness

## Slide 39: Conclusion I
The V-dependence of the statistical properties of the PEL can be quantified for models of liquids
Accurate EOS can be constructed from these information
Interesting features of the liquid state (TMD line) can be correlated to features of the PEL statistical properties
Connections between Dynamics and Thermodynamics

## Slide 40: Simple (numerical) Aging Experiment

## Slide 41: Aging in the PEL-IS framework
Starting
Configuration (Ti)
Short after
the T-change
(Ti->Tf)
Long time
Ti
Tf
Tf

## Slide 42: Evolution of eIS in aging (BMLJ)
W. Kob et al Europhys. Letters 49, 590 (2000).
One can hardly do better than equilibrium !!

## Slide 43: Which T in aging ?
F(T, Tf )=-Tf Sconf (eIS)+fbasin(eIS,T)
Relation first derived by S. Franz and M. A. Virasoro,
J. Phys. A 33 (2000) 891, in the context of disordered spin systems

## Slide 44: A look to the meaning of Teff

## Slide 45: How to ask a system its Tin t

## Slide 46: Fluctuation Dissipation Relation (Cugliandolo, Kurcian, Peliti, ….)
FS and Piero Tartaglia
Extension of the Fluctuation-Dissipation theorem to the physical aging of a model glass-forming liquid
Phys. Rev. Lett. 86, 107 (2001).

## Slide 47: Soft sphere
Support from the Soft
Sphere Model
F(V, T, Tf)=-TfSconf (eIS)+fbasin(eIS,T)

## Slide 48: From Equilibrium to OOE….
P(T,V)= Pconf(T,V)+ Pvib(T,V)
If we know which equilibrium basin the system is exploring…
eIS acts as a fictive T !
eIS, V, T
.. We can correlate the state of the aging system with an equilibrium state and predict the pressure
(OOE-EOS)

## Slide 49: Numerical Tests Liquid-to-Liquid
T-jump
at constant V
P-jump
at constant T
S. Mossa et al. EUR PHYS J B 30 351 (2002)

## Slide 50: Numerical Tests Heating a glass at constant P
T
P
time

## Slide 51: Numerical Tests Compressing at constant T
Pf
T
time
Pi

## Slide 52: Ivan New work ???

## Slide 53: Kovacs (cross-over) effect
Breaking of the out-of-equilibrium theory….
S. Mossa and FS, PRL (2004)

## Slide 54: Break -down - eis-dos From Kovacs

## Slide 56: Conclusion II
The hypothesis that the system samples in aging the same basins explored in equilibrium allows to develop an EOS for OOE-liquids depending on one additional parameter
Small aging times, small perturbations are consistent with such hypothesis. Work is ongoing to evaluate the limit of validity.
 This parameter can be chosen as fictive T, fictive P or depth of the explored basin eIS

## Slide 57: Perspectives
An improved description of the statistical properties of the potential energy surface.
 Role of the statistical properties of the PEL in liquid phenomena
 A deeper understanding of the concept of Pconf and of EOS of a glass.
 An estimate of the limit of validity of the assumption that a glass is a frozen liquid (number of parameters)
 Connections between PEL properties and Dynamics

## Slide 58: References and Acknowledgements
We acknowledge important discussions, comments, criticisms from P. Debenedetti, S. Sastry, R. Speedy, A. Angell, T. Keyes, G. Ruocco and collaborators
Francesco Sciortino and Piero Tartaglia
Extension of the Fluctuation-Dissipation theorem
to the physical aging of a model glass-forming liquid
Phys. Rev. Lett. 86 107 (2001).
Emilia La Nave, Stefano Mossa and Francesco Sciortino
Potential Energy Landscape Equation of State
Phys. Rev. Lett., 88, 225701 (2002).
Stefano Mossa, Emilia La Nave, Francesco Sciortino and Piero Tartaglia, Aging and Energy Landscape: Application to Liquids and Glasses., cond-mat/0205071

## Slide 59: Entering the supercooled region

## Slide 60: Same basins in Equilibrium and Aging ?