## Slide 1
Density anomalies and fragile-to-strong dynamical crossover
Peter H. Poole
Department of Physics
St. Francis Xavier University
Antigonish, Nova Scotia, Canada
and
Ivan Saika-Voivod (Roma)
Francesco Sciortino (Roma)
Unifying Concepts in Glass Physics III
Bangalore, June, 2004

## Slide 2: Two tetrahedral liquids silica water

## Slide 3: Thermodynamically similar: temperature of maximum density (TMD) in silica and water
From Angell and Kanno, Science (1976):
TMD of water and silica, scaled for comparison

## Slide 4
But dynamically different: silica is strong, water is fragile.
Angell’s classification of glass-forming liquids…
Adapted from Debenedetti and Stillinger, Nature (2001)
Water
Given the connection between dynamics and thermodynamic properties suggested by the Adam Gibbs relation…
…how can these two substances share such a rare thermodynamic behavior (a TMD), yet exhibit it in such different dynamical regimes?
TMD
TMD

## Slide 5: Molecular dynamics simulations of BKS silica
BKS silica pair potential: Van Beest, et al., 1990
Charged soft spheres; ignores polarizability, 3-body interactions
Long range forces evaluated via Ewald method.
PLUS, we add switching function to real-space part of potential.
Constant (N,V,E) molecular dynamics simulations
1332 ions (888 O, 444 Si)
See Saika-Voivod, et al., PRE (2004) for simulation details.

## Slide 6: Dynamics and the energy landscape in BKS silica
inflection
At high density, liquid remains fragile over observed range of T.
Horbach and Kob (PRB, 99) showed that at low density, liquid is fragile at high T, but becomes progressively more Arrhenius as T decreases.
At high density, inherent structure energy, eIS decreases rapidly, as found for BLJ liquid.
At low density, eIS inflects, suggesting the approach to a constant…
Saika-Voivod, et al., Nature (2001)
Saika-Voivod, et al., PRE (2004)

## Slide 7: Energy and specific heat of BKS silica
crystal
liquid
Beginning of fragile-to-strong crossover is accompanied by a specific heat anomaly in the total thermodynamic properties.
from eIS only
CV - (3/2)R
Saika-Voivod, et al., Nature (2001)
Saika-Voivod, et al., PRE (2004)

## Slide 8: Comparison of real silica and BKS phase diagrams
fragile
strong
strong
CV max
Pressure range of crystal stability fields is too low.
Temperature of melting lines too high; triple points up to 30% too high.
But topology is correct: BKS exhibits a silica-like phase diagram.
Yet…TMD is up to 170% too high (!)
Is the BKS TMD silica-like or water-like?
L = liquid
S = stishovite
C = coesite
Q = beta quartz
Saika-Voivod, et al., cond-mat (2004)

## Slide 9: Molecular dynamics simulations of ST2 water
ST2 water pair potential: Stillinger and Rahman (1974).
Five-site rigid molecule: one O atom, two H atoms and two “lone pair” sites.
Constant (N,V) molecular dynamics simulations with Berendsen thermostat.
1728 molecules
Equilibrated at 2633 state points.
Equilibration/production time is greater of 0.5 ns and time for msd to exceed 1.0 nm2.

## Slide 10: Isotherms of pressure vs volume for ST2 water
Cavitation: nucleation of gas bubble in stretched liquid
Liquid-liquid phase separation

## Slide 11: Why ST2 water?
TMD
liquid + gas
liquid
LDL
HDL
HDL+LDL
Has prominent TMD.
Like SW silicon (Sastry and Angell, 2003), has an explicit liquid-liquid phase transition. (PHP, Sciortino, Essmann, Stanley, 1992, 1993, 1997; Harrington, et al. 1997).
Like BKS silica, ST2 exhibits onset of fragile-to-strong crossover when passing into LDL region (Paschek and Geiger, 1999).
HDL = high density liquid
LDL = low density liquid
LDL
HDL

## Slide 12: Isobars of diffusion coefficient for ST2 water

## Slide 13: Radial distribution function for i-th nearest neighbours
Define RDF of an i-th nn as,
such that,
is the probability that an i-th nn atom is found at a distance between r and r+dr from a reference atom.
That is,
where g(r) is the usual RDF.
5
4
3
2
1
6
7
8

## Slide 14: Liquid-liquid phase transition in ST2 water
TMD
liquid + gas
liquid
LDL
HDL
LDL + HDL
HDL = high density liquid
LDL = low density liquid, is a random tetrahedral network (RTN) liquid, that forms cooperatively.
g5
blue
red
0.94 g/cm3
230 K

## Slide 15: Development of the RTN in ST2 water
TMD in ST2 water corresponds to T range in which 5th nn is expelled from 1st coordination shell
Minimum of pressure isochore corresponds to TMD
g5
g4
g6
Si-O i-th nn RDF’s
density=0.83 g/cm3

## Slide 16: Development of the RTN in BKS silica
As in ST2, TMD seen in BKS corresponds to T range in which 5th nn is expelled from 1st coordination shell
Minimum of pressure isochore corresponds to TMD
g5
g4
g6
Si-O i-th nn RDF’s
density=2.3 g/cm3

## Slide 17: Curvature at TMD
Density of BKS silica along P=-1.9GPa isobar, where density at TMD is 2.3 g/cm3
Both BKS silica and ST2 water have much sharper TMD’s than real silica

Density of ST2 along P=0 MPa isobar, where density at TMD is 0.93 g/cm3

## Slide 18: The story so far…
So…
Either BKS is just a poor model of real silica…i.e. too water-like.
Or, there are two TMD’s in real silica…
  “Configurational TMD”:
    At higher T, near onset of fragile-to-strong crossover
    “Water-like” TMD, involving emergence of RTN.
  “Vibrational TMD”:
    At lower T, well below fragile-to-strong crossover
    Viscous liquid version of TMD in (well-formed) amorphous and (perfectly-formed) crystalline tetrahedral networks.
    Ice Ih, a-SiO2, and perhaps LDA ice all have density maxima. (H. Tanaka, 2001)
“vibrational TMD”
Requires temperature of minimum density!
“configurational TMD”
TMD in BKS and ST2 are alike…
  Dynamically
  Structurally
  Thermodynamically
Both differ from TMD in real silica.

## Slide 19: A density minimum in BKS or ST2?
BKS silica
Density = 2.37 gm/cm3 isochore
From Horbach and Kob (PRB, 99)
ST2 water
P=80 Mpa isobar
From Paschek and Geiger (JPC, 99)

## Slide 20: Isochores of liquid ST2 water
LDL
HDL
?

## Slide 21: Density minimum and CV maximum in ST2 water
To confirm hint of a density minimum in N=1728 system, use N=216 to reach lower T in the same compute time.
We average each isochore over 40 independent runs, to reduce uncertainties.
inflection = CV max
inflection in energy

## Slide 22: Implications of a density minimum for the energy landscape
As system approaches the bottom of the landscape, configurational influences on thermodynamic properties fade, restoring positive expansivity.
Sciortino, La Nave and Tartaglia, PRL (2003): Assuming a Gaussian distribution of eIS, at most one density anomaly (a maximum) is possible…
So occurrence of a density minimum implies the breakdown of this assumption, as shown directly by Heuer (this conference).
bottom of the energy landscape

## Slide 23: Conclusions
RTN substances may exhibit several kinds of density anomaly:
  A high-T density maximum in the liquid phase driven by the initial formation of the RTN (e.g. real water, BKS silica).
  A density minimum in the liquid in the region of the fragile-to-strong crossover (e.g. ST2 water).
  A density maximum of vibrational origin in crystal and amorphous solid forms (e.g. ice Ih, a-SiO2, and perhaps LDA ice).
  A density maximum in the strong liquid regime…perhaps (mostly) vibrational in origin (e.g. real liquid silica).
Existence of a density minimum indicates that the assumption of a Gaussian distribution of inherent structure energies breaks down in the fragile-to-strong crossover region, as the system probes the bottom of the landscape.
So…water and silica are alike in that they both have density maxima, but the physical origins of these two TMD’s may be quite different.
Thanks to…